## Slide 1
ELI Summer School 28.8.2019
Advanced research using high intensity laser produced photons and particles (ADONIS), Reg. n.: CZ.02.1.01/0.0/0.0/16_019/0000789
Time-Resolved Ellipsometry in the Optical and VUV Region
Shirly Espinoza1, Steffen Richter1,
Mateusz Rebarz1 and Jakob Andreasson1,2
1 ELI Beamlines, Czech Republic
2 Chalmers University of Technology, Sweden
Supported by the European Regional Development Fund: ADONIS (CZ.02.1.01/0.0/0.0/16_019/0000789) and ELIBIO (CZ.02.1.01/0.0/0.0/15_003/0000447)
and by the National Science Foundation (DMR-1505172)

## Slide 2
OUTLINE
2
Introduction to ellipsometry
Ultrafast processes in Semiconductors
Time-Resolved Ellipsometry: NIR-NUV
Dynamics of the dielectric function on Germanium and InP after a a 1.55 eV (800 nm)
Magneto-Optical VUV Ellipsometer
28.08.2019

## Slide 3
L1
L3
HHG
opt. tables
3
E1 End stations and beam transport for Applications in Molecular, Bio medical and Material science
1
2
3, 4
5
1: MAC, AMO and Coherent diffractive imaging
2: ELIps, VUV magneto optical ellipsometry
3: and 4: TREX, X-ray diffraction and absorption. PR
5: Optical probes (SRS, TR-absorption, 1 and 2D IR, TR-SE)
and monochromator
28.08.2019

## Slide 4
What is Ellipsometry?
ELLIPSOMETRY is a method based on measurement of the change of the polarisation state of light after reflection at non normal incidence on the surface to study
28.08.2019
4

## Slide 5
Fresnel coefficients:
Amplitude ratio
Phase difference
Ellipsometric parameters
28.08.2019
5

## Slide 6
PSCA – Polarizer-Sample-Compensator-Analyzer
Fourier
Analysis
How to do ellipsometry?
28.08.2019
6

## Slide 7
How to analyze data?
n, k
We always need models to interpret the measurements
and to get physical parameters of the layers!
28.08.2019
7

## Slide 8
Ellipsometry is:
  Well known
  Non-destructive
  Precise
Ellipsometry gives:
  Refractive index (n)
  Extinction coefficient (k)
  Film thickness
  Surface roughness
  Anisotropy
  Retardation
  Phase difference
  Birefringence
 is extremelly sensitive to ultra thin layers
Sensitivity
0.01 A
What physical parameters can we get?
28.08.2019
8

## Slide 9
Pump-probe reflection spectroscopy
Pump-probe ellipsometry
28.08.2019
9

## Slide 10
Ultrafast processes in semiconductors
10
Applications:
  Fast electronics
  High speed optical switching
  Light harvesting
28.08.2019

## Slide 11
Ultrafast processes in semiconductors
11
Dielectric function response
28.08.2019
Notes: Change grey coding

## Slide 12
Dielectric function of Ge and InP
Indium Phosphide
1,55 eV pump
1,55 eV pump
Germanium
Bulk Ge with 29 Å oxide thickness
Bulk InP with 31 Å oxide thickness
12
Electronic structure of Ge and InP showing E1, and E1+D1
28.08.2019
Notes: We are probing the E1 transitions which occur at the L point of the Brillouin zone and in Ge they are split by spin orbit interactions, not in InP.

## Slide 13
L1
L3
HHG
opt. tables
13
E1 End stations and beam transport for Applications in Molecular, Bio medical and Material science
1
2
3, 4
5
1: MAC, AMO and Coherent diffractive imaging
2: ELIps, VUV magneto optical ellipsometry
3: and 4: TREX, X-ray diffraction and absorption. PR
5: Optical probes (SRS, TR-absorption, 1 and 2D IR, TR-SE)
and monochromator
28.08.2019

## Slide 14
Experimental Setup
14
28.08.2019
Notes: The lens has a rather long focal length and therefore has not a big impact in the polarization of the reflected beam.

## Slide 15
Experimental Setup
15
28.08.2019
Notes: The lens has a rather long focal length and therefore has not a big impact in the polarization of the reflected beam.

## Slide 16
Experimental Setup
16
28.08.2019
Notes: The lens has a rather long focal length and therefore has not a big impact in the polarization of the reflected beam.

## Slide 17
Experimental Setup
17
28.08.2019
Notes: The lens has a rather long focal length and therefore has not a big impact in the polarization of the reflected beam.

## Slide 18
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
18
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
28.08.2019
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 19
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
19
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
28.08.2019
From 0 to 2ps
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 20
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
20
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
28.08.2019
From 0 to 2ps
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 21
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
21
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2ps
28.08.2019
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 22
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
22
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2ps
28.08.2019
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 23
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
23
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2ps
28.08.2019
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 24
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
24
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2 ps
From 2 ps to 500 ps
28.08.2019
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 10^20 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 25
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
25
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2 ps
From 2 ps to 500 ps
28.08.2019
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 26
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
26
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2 ps
From 2 ps to 500 ps
28.08.2019
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 27
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
27
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2 ps
From 2 ps to 500 ps
28.08.2019
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 28
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
28
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)
From 0 to 2 ps
From 2 ps to 500 ps
28.08.2019
Notes: Real (top) and imaginary (bottom) parts of the transient pseudodielectric function of Ge (with 4.5 nm native oxide) versus photon energy during the ﬁrst 2 ps (left) and at later times (right) after photoexcitation of 1020 cm−3 electron-hole pairs with a pump photon energy of 1.55 eV.

## Slide 29
Dynamics of dielectric function of InP at 800 nm excitation (1.5 eV)
29
28.08.2019
Carrier concentration:
1020 cm-3
Penetration of pump: 220 nm
(350 um diam.)
Penetration of probe beams:
10 - 60 nm
(200 um diam.)

## Slide 30
Schematic Band Structure of Ge and InP
Excitation with 1.5 eV Pump Beam
Indium Phosphide
Germanium
27.05.2019
30
Notes: Schematic band structure of Ge showing optical interband transi-tions (red) from the heavy (hh), light (lh), and split-oﬀ (so) hole bands into the conduction band (CB) with 1.5 eV photoexcitation.
Electron-phonon coupling with multiple phonon modes (magenta) scatters the electrons to the L- and X-valleys, where they relax.
The pump pulse with 1.5 eV photons excites three different electron-hole populations through interband transitions
originating from the heavy, light, and split-o hole bands. The excess energy of these electrons (heavy holes) is up to
0.6 eV (0.1 eV), which corresponds to electron and heavy hole temperatures of 4600 K and 800 K, respectively

## Slide 31
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
31
27.05.2019
Excitation in G-valley -> Scattering of electrons from G to X -> Scattering of electrons from X to L
Reduction of CP amplitudes. Blocking of E1 transitions. Photoexcited electrons at L reduce the amplitude of E1 transitions. Time: From 0 to 2 ps.
Not much red shift (BGR and thermal increase through lattice heating).
Holes at G do not contribute to E1 transitions (no effect on spectra).
Appl. Phys. Lett. 115, 052105 (2019)
Notes: The temperature dependence of the E1 energy is about 􀀀0.4 meV/K (see Ref. 12) and therefore we expect an E1 red-shift due to heating of no more than 8 meV. The observed redshift, while dicult to quantify, is about 20 meV. We therefore conclude that lattice heating might be a signicant portion of the observed redshift. Within 500 fs, they scatter from the X-valley to the Lvalley, which is about 0.4 eV lower in energy. The nonequilibrium electron distribution in the L-valley partially blocks the E1 and E1 + 1 transitions (Pauli blocking), thus reducing the amplitude of the E1 and E1+1 peaks in the pseudodielectric function.
Because the electron temperature is still very high after 500 fs, Pauli blocking extends beyond 2.6 eV. At 2 ps, the electrons have cooled down signicantly and therefore the pseudodielectric function at 2.6 eV has recovered its equilibrium value. On the other hand, the carrier density has not changed yet, indicated by the reduced amplitudes of the E1 and E1 + 1 peaks.

## Slide 32
Dynamics of dielectric function of Ge at 800 nm excitation (1.55 eV)
32
27.05.2019
Full recovery takes about 500 ps
At around 2.6 eV the recovery is much faster
Above 3 eV weak time dependence
Appl. Phys. Lett. 115, 052105 (2019)
Notes: Between 2 ps and 500 ps, the E1 and E1 + 1 amplitudes recover. This means that the electron concentration falls below the measureable threshold, rst by Auger recombination and later by ambipolar diffusion and electron-hole pair (radiative or non-radiative) recombination.

## Slide 33
Dynamics of <e2> and <e1> in Ge at 800 nm excitation (1.55 eV)
27.05.2019
33
Initial drop: Band filling due to scattering G,X->L (observed E1 transitions)
Recovery: Diffusion and recombination
Oscillation with 10 ps time scale (0.1 THz).
Much too long for Ge optical phonon period (110 fs).
2.55 eV signal: Initial heating and cooling of carriers in L valley
Fermi-level singularity related to band filling (Xu C., et al. Phys. Rev. Lett. 118, 267402, 2017)
Notes: Change time scales: initial on left, recovery on right, maybe on log scale

## Slide 34
Example: ZnO thin film (30nm on SiO2), hom. pumped by 266nm “entire film homogeneously pumped” (1020cm-3)
Results: ZnO thin film
arXiv:1902.05832 (2019)

## Slide 35
Femtosecond timescale:
  immediate bleaching/ blocking of above-gap absorption (excitons)
  mid-gap absorption
  “fine structure”
EPC – exciton-phonon complex
X - exciton
X
EPC
Dynamics of <e2> and <e1>: ZnO thin film 266 nm excitation (4.66 eV)
arXiv:1902.05832 (2019)

## Slide 36
Picosecond timescale:
  recovery of above-gap absorption
  vanishing mid-gap absorption
  vis refractive index increasing again
Dynamics of <e2> and <e1>: ZnO thin film 266 nm excitation (4.66 eV)
arXiv:1902.05832 (2019)

## Slide 37
  electrons and holes cooling by scattering with phonons
  excitation VB-CB around Г point (electrons and holes carry excess energy)
  electrons thermalize by carrier-carrier scattering (blocking X and EPC absorption)
  holes scatter to the edges of Brillouin zone (IVB absorption)
  hot phonons slow down electron re-laxation through phonon reabsorption
  reduction of excited carriers (non-radiative Auger recombination and radiative recombination)
Dynamics of <e2> and <e1>: ZnO thin film 266 nm excitation (4.66 eV)
arXiv:1902.05832 (2019)

## Slide 38
L1
L3
HHG
opt. tables
38
E1 End stations and beam transport for Applications in Molecular, Bio medical and Material science
1
2
3, 4
5
and monochromator
1: MAC, AMO and Coherent diffractive imaging
2: ELIps, VUV magneto optical ellipsometry
3: and 4: TREX, X-ray diffraction and absorption. PR
5: Optical probes (SRS, TR-absorption, 1 and 2D IR, TR-SE)

## Slide 39
ELI Beamlines
39
HHG Beamline operating modes
1 HHG Beam
2 HHG Beams
Slide from Jaroslav Nejdl. ELI-BL RP2
Prepared for 2 beam options
2 color drive beam
2 independent HHG sources
Time-preserving VUV monochromatization
Off-plane gratings
Toroidal/ellipsoidal mirrors

## Slide 40
40
1 kHz driver | 6 mJ, 40 fs from 2018 | L1: 100 mJ, <20fs from 2020
Wavelength | 10 -120 nm | 5 -120 nm
Photons/shot | 106 to 109 | few 108 -1012
Dl/l | 10-2 | 10-2
Divergence | < 1 mrad | < 0.5 mrad
Spatial profile | Gaussian-like | Gaussian-like
Wavefront | l/10 | l/10
Duration | < 20fs | < 20fs
Polarization | Linear | Lin./Circ./Eliptical
Versatility / Tunability:
Several focusing geometries
Max. eff. at given wavelength range
Focusing chamber F- number 40-1000
Interaction chamber
IR rejection + diagnostics
Lasers
Slide from Jaroslav Nejdl. ELI-BL RP2
HHG Beamline

## Slide 41
41
Argon spectrum:
Neon spectrum
Pulse energy
  Pulse energy in Ar = 0.2 nJ, after 200 nm Al filter
  1e-6 efficiency of generation
HHG Beamline
Slide from Jaroslav Nejdl. ELI-BL RP2

## Slide 42
L1
L3
HHG
opt. tables
42
E1 End stations and beam transport for Applications in Molecular, Bio medical and Material science
1
2
3, 4
5
and monochromator
1: MAC, AMO and Coherent diffractive imaging
2: ELIps, VUV magneto optical ellipsometry
3: and 4: TREX, X-ray diffraction and absorption. PR
5: Optical probes (SRS, TR-absorption, 1 and 2D IR, TR-SE)

## Slide 43
VUV ellipsometer (“ELIps”)
43
Appl. Surf. Sci. 421, 378. (2017)
Commercial VUV ellipsometers
are currently available up to 140 nm (8.86 eV)6,7. For higher energies, the ellipsometer at MLS uses synchrotron light and has
a documented VUV operational energy range extending up
to 40 eV.
The ELIps instrument at the ELI Beamlines facility is the first user oriented endstation to study transient effects in the materials, in time scales from femtoseconds to picoseconds.

## Slide 44
44
Time-resolved VUV ellipsometry
27.05.2019
The ELIps use the VUV-High Harmonic light generated on
an Argon or Neon gas cell pumped by a 12 mJ, 15 fs, 1 kHz in-house-developed L1 ALLEGRA laser with central wavelength 830 nm.

## Slide 45
45
Time-resolved VUV ellipsometry
27.05.2019
The ellipsometer was tested as a rotating analyzer ellipsometer (RAE)

## Slide 46
46
Summary
Time-resolved spectroscopic ellipsometry allows direct observation of carrier excitation and relaxation of L-point electrons on a fs-ns timescale
Both 1.55 eV and 4.65 eV excitations show band-filling at the L-point in Germanium (E1 and E1 + D1)
In Indium Phosphide only 4.65 eV pump pulses can excite electrons to the L-valley. The electrons will scatter from L to G in less than 250 fs
Results on the VUV ellipsometry were obtained during the first user call
Workshop in Prague on November 11-13th, 2019
A new call for users will be open in Oct.-Nov., 2019
27.05.2019

## Slide 47
47
Acknowledgement
ELI RP4 and ELIBIO team
Steffen Richter
Mateusz Rebarz
Jakob Andreasson
Universität Leipzig
Oliver Herrfurth
Rüdiger Schmidt-Grund
Thank you for your attention!
27.05.2019
Università degli Studi di Padova
Fabio Samparisi
Luca Poletto
Fabio Frassetto
New Mexico State
University
Stefan Zollner
Carola Eminger